PRODUCT DESCRIPTION


LOCTITE® Product 7065 is a single component non-CFC solvent based formulation for cleaning and degreasing of surfaces to be bonded with Loctite adhesives. The product is FLAMMABLE. 





TYPICAL APPLICATIONS


Recommended as a final pre-assembly cleaning treatment for all surfaces to be bonded with LOCTITE®  adhesives. Because of its high solvent power it is also very effective in other degreasing or parts cleaning applications.





LIQUID PROPERTIES�
Typical Value�
�
Chemical Type�
Isoparaffin(100% w/w�
�
Appearance�
Light Blue �
�
Specific Gravity @ 25(C�
0.76�
�
Viscosity @ 25(C, mPa.s (cP)�
2�
�
Corrosivity�
none�
�
Drying time @ 20(C, minutes�
20 - 40�
�
Flash Point (COC), (C�
56�
�
TLV, (ACGIH), ppm�
300�
�



(	Isoparaffin is an environmentally friendly solvent.


It has zero Ozone Depletion Potential.


Conforms to German WGK, category zero.








TYPICAL  PERFORMANCE


This product is primarily a cleaning agent. The cleaner has no effect on the speed of cure or final strength of LOCTITE®  adhesives other than providing a clean surface for good adhesion and adhesive cure.  Unclean or partially cleaned surfaces can affect adhesive performance.





HANDLING PRECAUTIONS


Cleaner must be handled in a manner applicable to flammable materials and in compliance with relevant local regulations. For example, special care must be taken to avoid contact of the product or its vapour with naked flame or any electrical equipment that is not flame proofed.





Avoid prolonged or repeated skin contact.





Use only in a well ventilated area.








GENERAL INFORMATION


For safe handling information on this product, consult the Material Safety Data Sheets, (MSDS).





This cleaner contains a solvent which can affect certain plastics or coatings. It is recommended to check all surfaces for compatibility before use.


�Directions for use


Clean surfaces to be bonded by wiping surfaces with paper towel soaked with cleaner.





Re-wipe surfaces when still wet with a clean paper towel to ensure heavy contamination and excess solvent is removed.





Repeat cleaning of surfaces if  deemed necessary.





Allow the solvent time  to evaporate until the surfaces are completely dry





Apply the LOCTITE® adhesive immediately after drying and assemble bond.





Storage


This cleaner is classified as being FLAMMABLE and therefore must be stored in an appropriate manner and in compliance with relevant regulations.  Do not store near oxidising agents or combustible materials.





Product shall be ideally stored in a cool, dry location in unopened containers at a temperature between 8(C to 28(C  (46(F to 82(F) unless otherwise labelled.   Optimal storage is at the lower half of this temperature range.  To prevent contamination of unused product, do not return any material to its original container.  For further specific shelf life information, contact your local Technical Service Centre.





Note


The data contained herein are furnished for information only and are believed to be reliable.  We cannot assume responsibility for the results obtained by others over whose methods we have no control.  It is the user's responsibility to determine suitability for the user's purpose of any production methods mentioned herein and to adopt such precautions as may be advisable for the protection of property and of persons against any hazards that may be involved in the handling and use thereof. In light of the foregoing, Loctite Corporation specifically disclaims all warranties expressed or implied, including warranties of merchantability or fitness for a particular purpose, arising from sale or use of Loctite Corporation’s products.  Loctite Corporation specifically disclaims any liability for consequential or incidental damages of any kind, including lost profits.  The discussion herein of various processes or compositions is not to be interpreted as representation that they are free from domination of patents owned by others or as a license under any Loctite Corporation patents which may cover such processes or compositions.  We recommend that each prospective user test his proposed application before repetitive use, using this data as a guide.  This product may be covered by one or more United States or foreign patents or patent applications.














				TDS  7065  February 23 1994








	


		Loctite is a Registered Trademark of Loctite Corporation, Hartford, CT 06106





��			Technical Data Sheet


Research, Development & Engineering			Product 7065


Tallaght Business Park,


Dublin, Ireland			Worldwide Version, October 1995











NOT FOR PRODUCT SPECIFICATIONS


THE TECHNICAL DATA CONTAINED HEREIN ARE INTENDED AS REFERENCE ONLY. 


PLEASE CONTACT LOCTITE CORPORATION  QUALITY DEPARTMENT FOR ASSISTANCE AND RECOMMENDATIONS ON SPECIFICATIONS FOR THIS PRODUCT.


ROCKY HILL, CT    FAX: +1 (860)-571-5473                  DUBLIN, IRELAND    FAX: +353-(1)-451 - 9959


	�














