|  | Zinc Spray |
| --- | --- |

DESCRIPTION

Loctite 7800 provides a corrosion protective coating at room temperature on ferrous metals

APPLICATION

Loctite product 7800 is used to touch up metal parts after welding and to provide long-term protection of metal assemblies.  It is also used to restore protection to repaired galvanised parts, e.g. crash barriers, tubes, flanges, tanks, panels, etc.

DIRECTIONS FOR USE

Shake well before use.

Spray on to clean parts, where possible, from a distance of 20 - 30 cm to give a uniform film.

PRODUCT PROPERTIES

| Base | Zinc in Resin |
| --- | --- |
| Colour | Grey |
| Odour | Light |
| Density @ 20ºC, g/ml NFT 60 101/ISO 3675/DIN 51 757 | 0.8 |
| Viscosity @ 20ºC, mm²/s NFT 60 100/ISO 3104.3105/ DIN 51 562 | 10 |
| Flash point, ºC NFT 60 118/DIN ISO 2592 | Not Applicable |
| Tack free time (Dry to touch), seconds | 20-60 |
| Cure time, hours for handling strength for functional strength Spirit content, % | 1 24 10 |
| AEROSOL CHARACTERISTICS |  |
| Propellant | CO2 |
| Weight, % | 3 |
| PERFORMANCE |  |
| Salt Spray Test (5%, 35ºC) NFX 41002 (Ri NFT 30 071/ISO 4628) | 0 - 72hr Ri 0 72 - 120hr Ri 1 120 - 168hr Ri 2 168 - 216hr Ri 3 216 - 264hr Ri 4 after 264hr Ri 5 |
| Recommended Operating Temperature Range, ºC | -50 to +550 |